## Slide 1: Spinodal Decomposition Benchmarks

## Slide 2: Purpose of This Set of Models
To exemplify and validate the use of COMSOL Multiphysics® for modeling and simulation with the phase field method
Many processes in the mesoscale can be described using this method
Several codes have been developed in the scientific community
  These codes are often benchmarked against a set of standard benchmark problems
The Phase Field interface in COMSOL Multiphysics is applicable to these problems
  The models in this presentation define and solve three standard benchmark problems for spinodal decomposition

## Slide 3: Spinodal Decomposition
Spinodal decomposition describes phase separation in a two-phase system
The atomic fraction of a solute () follows the Cahn-Hilliard equation
where is the solute’s mobility, is the chemical free energy density, and is the gradient energy coefficient
The total free energy of the system is expressed as follows:

## Slide 4: Problem 1(a-b) specifications
A 2D square domain with a side length of 200 meters
A simple polynomial form is chosen for the chemical free energy density:
Parameter values: , , , ,
Interfacial energy:
Initial condition for is
Problem (a) employs periodic boundary conditions, whereas problem (b) prescribes no-flux conditions
A. Jokisaari, P. Voorhees, J. Guyer, J. Warren, and O. Heinonen. Benchmark problems for numerical implementation of phase field models. Computational Materials Science 126, 139-151 (2017).
Note: the original benchmark does not specify units. In order to clarify the physics, we have appended SI units to all quantities.

## Slide 5: Problem 1(c) specifications
In the third benchmark, a T-shaped geometry is used
The T-shape is composed of two attached rectangles, both having a length of 100 meters and width of 20 meters
The same no-flux boundary conditions are used as in 1(b)
T-shaped geometry drawn in COMSOL Multiphysics®.

## Slide 6: Implementation
Problem is solved using the Phase Field interface
The solved equation is expressed as
Comparing this equation to the Cahn-Hilliard equation allows us to derive the correct expressions for , , and
The boundary condition Outlet provides the natural no-flux condition
The problem is nonlinear and exhibits both fast and slow dynamics:
  Adaptive time-stepping with a small initial step and tightened tolerance is used
  The tolerance in the Newton method is also tightened

## Slide 7: Problem 1(a) results

## Slide 8: Problem 1(b) results

## Slide 9: Problem 1(c) results

## Slide 10: Conclusions
The Phase Field interface was used to solve three benchmark problems
An equilibrium state of spinodal decomposition was reached in all three cases and the influence of boundary conditions is clearly visible
The total free energy was plotted versus time
The results are in line with those published by the phase field community