## Slide 1: Shape Memory Alloy examples
Notes: You can use the heading from the application documentation for the title.

## Slide 2: Background and Motivation
Shape memory alloys properties are based on transformations between austenite and martensite phases.
Transformations can be induced thermally or mechanically.
The main phenomena in shape memory alloys are pseudoelasticity and shape memory effect.

## Slide 3: Thermal Transformation
The phase transformation is described by the martensite volume fraction variable x.
When the material in its austenite phase is cooled, the martensite transformation starts at Ms temperature and ends at Mf.
When the martensite is heated the austenite transformation starts at As and end at Af.
0
1
Mf
Ms
As
Af
x
T
Austenite
Martensite

## Slide 4: Pseudoelasticity
At high temperature the austenite transforms to martensite under mechanical loading. The (s,e) graph shows inelastic behavior.
Once transformation is completed the material behaves linearly in martensite phase.
When the loading is decreased the material transforms back to austenite and recovers its initial shape.
s
e
Martensite
Austenite

## Slide 5: Shape Memory Effect
heating
At lower temperature the austenite transforms to martensite under mechanical loading as well.
When the loading is decreased the material stays in its martensite phase and residual deformation remains.
The austenite phase is retrieved by heating the material. The material then recovers its initial shape.
s
e
Martensite
Austenite

## Slide 6: Pseudoelasticity: Parametric model
The model used for pseudoelasticity is a cylinder submitted to uniaxial loading.
2D axisymmetric geometry is used.
A parametric study is performed to study the material at several temperatures: 328 K, 308 K, 276K, and 260 K.
 | Austenite | Martensite
Young’s modulus | 55 GPa | 46 GPa
Poisson’s ratio | 0.33 | 0.33
Heat capacity at constant pressure | 400 J/(kg.K) | 400 J/(kg.K)
Clausius-Clapeyron coefficient | 7.4 Mpa/K | 7.4 Mpa/K
Transformation start temperature | 270 K | 245 K
Transformation finish temperature | 280 K | 230 K
Maximum transformation strain | 0.056 | 
data taken from D.C. Lagoudas, Shape Memory Alloys, Modelling and Engineering Applications, Springer 2008

## Slide 7: Pseudoelasticity: Results
For high temperatures (328 K, 308 K) a pseudoelastic behavior is seen, with return to initial state
At 276 K (As<T<Af) the reverse transformation is not complete at zero stress, so residual deformations remain.
At 260 K (T<As) the reverse transformation has not started. The material is purely martensite and the residual strain is maximal.
Stress-strain curves for parametric temperature
Martensite volume fraction vs pseudo-time parameter

## Slide 8: Pseudoelasticity: partial transformation
On this model a prescribed displacement is applied.
The material is loaded to a fixed maximal displacement, then decreased to 40%, increased to 80%, and finally decreased to 0.
It induces an “internal loop” in the stress-strain graph.
Prescribed displacement
Martensite volume fraction
Stress-strain graph

## Slide 9: Shape Memory Effect
In this model the temperature is initially lower than the austenite start temperature. A stress cycle is applied and then the temperature is increased.
The unloading does not induce reverse transformation. It occurs only when the temperature is increased. At the same time the residual strain are decreased and the material recovers its initial shape.
Loading: stress and temperature
Martensite volume fraction
Stress-strain graph